## Slide 2: History
Started in 2012
Philosophy:
High efficiency biomass to charcoal
Robust and simple technology
No hazardous emissions
Affordable production costs

## Slide 3: Philosophy
Robust and simple technology
No heavy equipment for loading/unloading
Most construction work on location
Construction materials readily available
No advanced process control equipment

## Slide 4: Philosophy
High efficiency
Heating (combustion) separated from carbonisation
Drying and carbonisation separated
Energy content volatiles used for process heating

## Slide 5: Philosophy
No hazardous emissions
- Prevention of emissions of black vapours by combustion in wood stove
- Health problem workers and environmental
problem avoided

## Slide 6: First design

## Slide 7: Demo plant in Bosnia

## Slide 10: Results tests

## Slide 11: Results tests
Long drying time
Efficiency > 35%
After start-up process heat supply from volatile; no emissions of volatiles
Good quality charcoal
Caloric value charcoal: 30-32 MJ/kg
Temperature flue gases > 100 oC

## Slide 12: Results tests
Top loading less practical
Cooling outside reactor to decrease production time one cycle
Separate and simultaneous drying with flue gases

## Slide 13: Improved design
Front loading with reactors (3,5 m3 each)
Start-up with wood stove
Volatiles are burned in wood stove
Two furnaces: one for drying and one for carbonisation
Alternating use of reactors

## Slide 14: Improved design

## Slide 15: Principle

## Slide 19: Production full size module
Two furnaces each with four reactors
14 m3 volume carbonisation per batch
1.000-1.100 kg charcoal per batch
2-3 batches per day (depending on type of biomass, particle size, moisture content etc.)

## Slide 20: Program demo-plant 2015
Optimize time and temperature vs. quality charcoal
Operational protocol
Tests with rice hulls and sugar cane
Tests with peat
Other biomass